## Slide 1: Introduction : Research Objective
I
Taking 1 Month↑ & High Costs
Scan Spacing
Scan Path
Cooling Time
Scan Speed
Scan Power
Scan Length
Building Direction
>200 $/kg
Trial-and-error efforts
About 200 $/work
>150 $/work
Issues
Quality assurance
Poor quality
Property degradation
Powder
Consumable
Post processing
Broad impacts from the research
Quality & property
High-quality & property products
Printability map
In-depth investigation

## Slide 2
최종 목표: 오버샘플링한 데이터 기반 2D/3D 그래프 제작 & Correlation matrix 제작

## Slide 3
Scan speed | Laser power | Line spacing (s) | Layer thickness (t)
mm/s | W | mm | mm
1st 변수
1st Objective (2nd 변수): 1st 변수에 영향을 받음
Melt pool size (용융풀-녹은 형상의 치수) |  | 
Width | Depth | Height
Line spacing / H_max | Keyholing
 | (Depth/width)
Melt pool size 기반 Dimensionless parameter
Spattering (파우더/용융금속이 튀는 것) | Denudation width: Multi-layer (주변 금속분말을 날려버리는 정도) | Surface roughness (Ra, um)
(area) |  | 
목적: 1st 변수에 따른 품질/물성 예측 & 최적화
2nd Objective (3rd 변수): 2nd 변수에 영향을 받음
Relative density
(1-Porosity)
%
3rd (Final) Objective: (물성의 경우 3rd 변수에 영향을 많이 받음)+2nd 변수에도 영향을 받음
Hardness, Tensile Properties, Dimensional Accuracy, Productivity, Deformation, Overmelting depth
물성
품질
품질 (기공율), Relative density 99%일 경우 기공율(Porosity) 1%
Microscale  복잡한 현상들
Macroscale  파트를 만들 때 품질/물성
Spatter가 많이 튈수록(값이 클수록) 품질이 안 좋음
Denudation width가 클수록 품질이 안 좋음
Surface roughness가 클수록 품질이 안 좋음
주요 변수
에너지가 높은 경우: 결함
에너지가 낮은 경우: 결함

## Slide 4
Process-related physical metallurgical phenomena
2. Powder melting
Particle-sized denudation
1. Laser-powder interaction
Surface energy induced force
4. Denudation & Spattering
Extensive denudation
Evaporating force
Heat flux
Most of the heat flux move to bottom of the molten pool
Melt pool flow
Tail
Tailed
5. Melt pool solidification
Microstructure
Surface roughness
Residual stress
Effective layer thickness by shrinkage
3. Melt pool formation

## Slide 5
Conduction mode
Science 363.6429 (2019): 849-852.
Heat flux
Most of the heat flux move to bottom of the molten pool
Melt pool flow
Tail
Tailed
J shape morphology
Scan speed ↑
Keyhole
Humping
Keyhole induced pores
High Ev
P: 250 W
Vs: 400 mm/s
P: 250 W, Vs: 800 mm/s
Dl: 0.08 mm, Dt: 0.04 mm
Round shape (entrapped gas)
Ev: 97.7 J/mm3
Metallurgical pore
200
Keyhole induced pore
Lack of fusion
Low Ev
P: 250 W
Vs: 2000 mm/s
P: 180 W, Vs: 800 mm/s
Dl: 0.08 mm, Dt: 0.04 mm
Elongated and
irregular shape
Ev: 70.3 J/mm3
200
Lack of fusion
Shallow quasi-semicircular shape
Heat flux
Evaporating pressure
Melt pool dynamics and subsequent defects
Defect prediction & mitigation
Keyhole mode
High laser power

## Slide 6
Denudation and spattering induced by powders-melt pool interaction
Metal vapor flow
Shear flow of gas
by metal vapor jet
Outward evaporation
Inward vortex flow
Spatter
Powders-melt pool interaction
Denudation zone
Discontinuous and non-uniform
melt pools
Balling, pores, inclusion, rough surfaces
Poor as-printed qualities
Denudation & Spattering phenomena
[1]
50 W & 0.1 m/s
100 W & 0.5 m/s
200 W & 1 m/s
Forward ejection
Upward ejection
Backward ejection

## Slide 7
1. 오버샘플링  노이즈 데이터 제거 & 보충 (Follow up) 2. 이미지 기반 용융풀 예측 연구 – AI (Study) : 이미지 기반 용융풀의 치수(너비, 깊이, 높이)/면적 3. 열화상 카메라 기반 스패터 예측 연구 – AI (Study)

## Slide 8
1. 오버샘플링  노이즈 데이터 제거 & 보충 (Follow up) 2. 이미지 기반 용융풀 예측 연구 – AI (Study) 3. 열화상 카메라 기반 스패터 예측 연구 – AI (Study) : 동영상 이미지 학습 기반 공정조건별 스패터 양/거리/방향 예측
* 업무: 2&3번 관련 AI 모델 조사/파악  적용 (데이터 작업)
Notes: 설명: ~~

## Slide 9
Representative data of single tracks
Laser power↑ & Scan speed↓
Width↑ & Depth↓
200 mm/s
400 mm/s
600 mm/s
800 mm/s
1000 mm/s
1200 mm/s
1400 mm/s
1600 mm/s
1800 mm/s
2000 mm/s
Scan speed
Laser power: 50-500 W (at 50 W intervals)
Scan speed: 200-2000 mm/s (at 200 mm/s intervals)
Layer thickness: 0-120 μm (at 20 μm intervals)
Line spacing: 0-50% overlap rate
Width
Depth

## Slide 10
Laser power & Scan speed & Layer thickness에 따른 용융풀 너비/깊이/높이 수식모델
변수: Laser power & Scan speed & Layer thickness
목적함수: 용융풀 너비/깊이/높이 수식모델
e.g. 용융풀 너비=지수함수꼴 (Laser power, Scan speed, Layer thickness 계수)
e.g. 반응표면분석법(Polynominal)
변수: Power 크고, Speed 작고, Thickness 작을 때 목적함수: 용융풀 치수(너비, 깊이) 커짐
오버샘플링(AI)
Regression 기반 수식모델 구축

## Slide 11
Laser power & Scan speed & Layer thickness에 따른 용융풀 너비/깊이/높이 수식모델
변수: 용융풀 너비/깊이/높이 수식모델 + Line spacing
목적함수: 밀도
변수: 용융풀 너비/깊이/높이 수식모델 + Line spacing
목적함수: 밀도
변수: Laser power & Scan speed & Layer thickness
목적함수: 용융풀 너비/깊이/높이 수식모델
변수: Laser power & Scan speed & Line spacing & Layer thickness
목적함수: 밀도

## Slide 12
금속 3D 프린팅: 품질/물성 제어 어려움
이유) 장비/공정조건/소재에 따라 다 다르기 때문에
공정조건에 따른 용융풀/품질 DB – Stainless steel
Titanium 소재  오버샘플링  전이학습  데이터 기반 역으로 추정(왜 이렇게 달라지는지? 분석, 가이드라인)